SELENIUM MOBILITY IN COAL AND OVERBURDEN

IN CENTRAL APPALACHIA1

R.R. Maggard2

Abstract: The occurrences of low levels of Selenium (<50 µg/l) are continuing to be the bane of both regulatory and industry in the southern coal fields of West Virginia. This issue was first brought to the attention of the industry as a result of data gathered as part of the Mountaintop Mining Environmental Impact Study in 2002. The current chronic water quality standard in West Virginia of 5 µg/l is considerably less than the values found downstream of some coal mining sites. As a result of these situations, the West Virginia Division of Mining and Reclamation implemented an extremely conservative geochemical sampling and analysis plan with an associated special materials handling plan under the auspices of guidance in January 2008. The author presented concerns about the exact path (mobility) in which the selenium actually becomes part of the water column in a paper presented at this same symposium in 2004. Since that time (5 years), the regulatory agencies have done little to develop a realistic sampling and analytical procedure to determine the actual path of how selenium becomes part of the water column.

Additional key words: Mountaintop Mining, Valley Fill, Geochemical Analysis, Total Sulfur, Pyritic Sulfur, Acid Base Accounting, Neutralization Potential, Potential Acidity, Paste pH, Selenium Mobility, Leaching Procedures

________________________________________________________________

1 Paper presented at the 2008 Annual Meeting of the West Virginia Mine Drainage Task Force, Morgantown, WV March 31 – April 1, 2009

2 Randall Maggard, Manager of Environmental Compliance, Argus Energy WV, LLC, P.O. Box 200 Dunlow, WV 25511

3 Publication in these proceedings does not prevent author from publishing their manuscripts, whole or in part, in other publication outlets.

INTRODUCTION

Typically more common contaminants like iron, manganese, and aluminum are more of a concern with coal mine discharges than substances like selenium. After the passage of SMRCA (Surface Mine Reclamation Control Act) the issues of acid mine drainage (AMD) became a primary concern and even led to the formation of the very task force hosting this symposium. A very dedicated and intelligent group of individuals representing practically all the stakeholders have since made great strides in developing methods to both predict, prevent and remediate typical AMD. But the methods to deal with selenium have taken a very different path.

First we did not simply require the analysis of iron for the entire geologic column and simply conclude that the “special handling” of all iron bearing strata would prevent the formation of AMD. The reason for that was simply we knew we would find iron in all of the samples. After careful studies and discussions it was determined that it was the pyritic iron that was most problematic, not all of the iron in the strata. So to develop a more realistic approach to selenium we need to take a different route.

OBJECTIVES

The purpose of this paper is to share the results of several studies to determine the actual mobility of selenium in the strata and which stratagraphic units may be problematic and need special attention. The focus of this analytical work is more concentrated on using the typical acid base analysis in conjunction with selenium analysis and several leaching techniques to better determine the potentially problematic strata in regard to selenium solubility.

METHODOLOGY FOR SELENIUM ANALYSIS

The solid samples (coals, overburdens) were composites collected using methods approved for coals and soils. The samples were prepared for analysis using SW-846 Method 3050B. This is an acid digestion involving nitric acid, hydrogen peroxide and the application of heat. After digestion, the resulting extract is then analyzed for selenium using method SD 7740. This method utilizes Graphite Furnace Atomic Absorption Spectroscopy. The minimum detection level for this procedure is 0.5 mg/kg. Some of the samples were re-analyzed using the Hydride AF method which is described in further detail in the appendix.

METHODOLOGY FOR SELENIUM LEACHABLITY

During previous studies and review of data, several trends were noted.

- Selenium solubility and occurrences in mine discharges appear to be related to neutral to higher pH with water of moderate to high alkalinity.

- Selenium has been known to be associated with sulfur in overburden and coal samples.

- Occasionally, selenium detected in shale samples that exceed the 1 mg/kg established by the WVDEP for special handling do not contain detectable or contain very low levels of pyritic sulfur.

As a result of the above mentioned trends, several methods were developed to determine the circumstances which might facilitate maximum selenium leachability under somewhat natural conditions but in a reproducible and simple expedited procedure.

Procedures

First various samples of a core hole were chosen based on the varying combinations of conditions which exist in the various rock types:

- Sample #5 was selected with barely detectable pyritic sulfur of 0.01 percent with a net neutralization potential of 4.24 and a paste pH of 7.6 and a selenium value of 2.19 mg/kg by the Hydride AF Procedure,

- Sample #8 was selected with below detectable value of pyritic sulfur <0.01 percent with a net neutralization potential of 13.73 and a paste pH of 7.7 and a selenium value of 1.02 mg/kg by the Hydride AF Procedure            right at the threshold of the WVDEP special handling criteria of 1 mg/kg.

- Sample #14 was selected with a 0.07 value for pyritic sulfur with a net neutralization potential of 1.86 and a paste pH of 7.6 and a selenium value of 0.75 mg/kg which is below the WVDEP threshold and was analyzed by the Hydride AF Procedure,

- Sample #12C was selected with a below detectable value of pyritic sulfur <0.01 percent with a net neutralization potential of 0.91 and a paste pH of 6.2 and a selenium value of 4.92 mg/kg. This sample was analyzed by the GFAA Procedure.

- Sample #16C was selected with an easily detectable value of pyritic sulfur of 0.82 percent with a deficiency of neutralization of 36.74 and a paste pH of 3.4 and a selenium value of 9.46 mg/kg. This sample was analyzed by the GFAA Procedure.

Leaching Method Number One

During this procedure each of the samples were subjected to a one hour exposure to the leaching solution while shaken. The sample size was 2 grams with a 50 ml of leaching solution which ranged from a pH of 2.0 (adjusted H2SO4) to a pH of 10.0 (adjusted with CaO).

At the end of one hour of leaching, the resultant extract was measured for pH and analyzed for total selenium, aluminum, iron, manganese, calcium and magnesium.

As you can see by reviewing Table 1 all samples extracted measurable selenium from a low of about 4 µg/l to a high of about 82 µg/l. Some variabilities can be noted. Sample No. 5 had about the same levels as Sample No. 16C which had about 4 times the selenium in the solid sample. Also note that the maximum solubility seemed to occur around a pH of 9. The soluble iron remaining in the extract also seemed to play a role.

Leaching Method Number Two

This method was developed to determine the relationship between sample size and volume of extract.

During this procedure, Sample No. 14 was chosen because it had the lowest measurable value of selenium in the original solid sample (0.75 mg/kg). The sample sizes ranged from 0.5 grams to 50 ml of extract at a pH of 9 (which exhibited the highest numbers in the previous procedure) to 2 grams to 50 ml. We were also concerned about extracted solids contaminating the resultant extract so each run was duplicated using a 0.45 µm filter and a 0.20 µm filter to note any differences.

The values in the extract ranged from about 2 µg/l to a high of about 8 µg/l.  The last runs of 2.0 grams to 50 ml with the same sample yielded between 7 and 8 µg/l in the extraction. As you can see in Figure No. 1 the values appear to be practically linear in regards to sample size and extract.

Prevention and Treatment

A last minute procedure was performed just prior to completing this paper which involved the addition of dried AMD sludge to various overburden and coal samples to determine if iron in the AMD sludge could prevent or reduce the mobility of selenium. This idea was proposed by Dr. P. Ziemkiewicz. The results appear promising, using the same leaching procedure previously described with a 10 percent addition of dried AMD sludge by weight reduced soluble selenium levels from 17 to 33 percent. This data is present in Figure 2.

Conclusions

The solubility and mobility of selenium as a result of various coal extraction methods can be highly variable depending on the geochemical characteristics of the parent source rock. The author feels that pyritic sulfur content is important and may play a role in inhibiting the solubility or mobility of selenium in the water column. Others (Lovett and Ziemkiewicz) have previously noted the effects of iron in the system to both be effective in the treatment and possible prevention of selenium being mobilized and discharged from coal extraction sites.

The author feels more efforts need to be made to better understand the mobility issue so more cost effective and practical methods of special handling can be developed and implemented.

Currently additional leaching studies are being conducted by the author to better understand the circumstances of selenium solubility and mobility and its prevention in the Southern Appalachia coalfields.

Acknowledgements

The author wishes to acknowledge the contributions and hard work made in preparation of this paper by Sharon Cornette, Emily Lawson and Waylon Bryant of P&A Engineers and Consultants and Tim Keeney and Ivan Leef of REI Consultants, Inc.

References

Bryant, G., S. McPhilliamy, H. Childers. 2002. A Survey of Water Quality of Streams in the Primary Region of the Mountaintop/Valley Fill Coal Mining, October 1999 to January 2001, USEPA Region III, Wheeling, WV.

Caruccio, F. T. and G. Geidel 1996, “Acid Mine Drainage: The Laboratory and Field Settings”, Workshop 6- 13th Annual Meeting of the American Society for Surface Mining and Reclamation, Knoxville, TN, 58p.

Faulkner, B. and J. Skousen. 1991, Field Experiences in Acid Prevention”, Proceedings - 12th Annual West Virginia Surface Mine Task Force Symposium.

Faulkner, B. and Skousen, J. 1991, “Field Trials in Acid Treatment” 12th Annual West Virginia Surface Mine Drainage Task Force Symposium.

Gayla, T. 1994, Personal Communication West Virginia Division Environmental Protection, Logan, WV

Lovett, R. 1991, “Chemistry of Manganese in Acid”, Proceedings – 12th Annual West Virginia Surface Mine Drainage Task Force Symposium.

Lovett, R. 2007, “Results of Bench-Scale Selenium Treatment Trials”, 28th Annual West Virginia Mine Drainage Task Force Symposium

Maggard, R. 2004, “The Occurrence and Impacts of Selenium in Aquatic Systems Downstream of a Mountaintop Mining Operation in Central Appalachia”, 25th Annual West Virginia Surface Mine Drainage Task Force Symposium.

Morrison, J.L. and B.E. Scheetz 1994, “Overburden Characterization: An Examination of the Neutralization Potential Determination and Identifying Potential Sources of Manganese”, PEDAFR-486-043, The Materials Research Laboratory, Pennsylvania State University

Sobek, A.A., Schuller, W.A., Freeman, J.R. and Smith, R.M. – 1978, Field and Laboratory Methods

USEPA. 2003. Mountaintop Mining/Valley Fills in Appalachia Draft Programmatic Environmental Statement. EPA Region #, Philadelphia, PA.

Wiram, V.P. 1992, “Siderite Masking A Factor to Consider in Overburden Acid-Base Balancing”, Proceedings – 13th Annual West Virginia Surface Mine

Ziemkiewicz, P. 2009, Personal Communication, West Virginia University, Morgantown, WV

| Table 1. Argus Energy Leach Study 0810K03 |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | mg/l |  |  |  |  |  |  |  |  |
| ABA Sample ID |  | Final pH |  | Selenium | Aluminum |  | Iron | Manganese |  | Calcium | Magnesium |  |
| #5, pH 2.0 |  | 2.18 |  | 0.0173 | 3.03 |  | 20.1 | 0.337 |  | 29.0 | 10.2 |  |
| #5, pH 3.0 |  | 3.98 |  | 0.0181 | 0.185 |  | 2.26 | <0.10 |  | 14.9 | 5.23 |  |
| #5, pH 4.0 |  | 8.56 |  | 0.0175 | <0.10 |  | <0.10 | <0.10 |  | 1.01 | 0.411 |  |
| #5, pH 5.0 |  | 8.85 |  | 0.0192 | <0.10 |  | <0.10 | <0.10 |  | 0.681 | 0.290 |  |
| #5, pH 6.0 |  | 9.01 |  | 0.0196 | <0.10 |  | <0.10 | <0.10 |  | 0.689 | 0.278 |  |
| #5, pH 7.0 |  | 8.78 |  | 0.0201 | <0.10 |  | <0.10 | <0.10 |  | 0.652 | 0.289 |  |
| #5, pH 8.0 |  | 8.91 |  | 0.0212 | <0.10 |  | <0.10 | <0.10 |  | 0.674 | 0.292 |  |
| #5, pH 9.0 |  | 9.07 |  | 0.0225 | <0.10 |  | <0.10 | <0.10 |  | 0.934 | 0.388 |  |
| #5, pH 10.0 |  | 9.45 |  | 0.0204 | <0.10 |  | <0.10 | <0.10 |  | 1.27 | 0.515 |  |
| #8, pH 2.0 |  | 2.32 |  | 0.0056 | 6.29 |  | 124 | 5.9 |  | 63.9 | 17.1 |  |
| #8, pH 3.0 |  | 5.32 |  | 0.0064 | 0.147 |  | 1.98 | 0.684 |  | 21.0 | 6.33 |  |
| #8, pH 4.0 |  | 9.30 |  | 0.0067 | <0.10 |  | <0.10 | <0.10 |  | 2.98 | 1.11 |  |
| #8, pH 5.0 |  | 9.70 |  | 0.0076 | <0.10 |  | <0.10 | <0.10 |  | 2.61 | 0.945 |  |
| #8, pH 6.0 |  | 9.67 |  | 0.0076 | <0.10 |  | <0.10 | <0.10 |  | 1.98 | 0.734 |  |
| #8, pH 7.0 |  | 9.73 |  | 0.0069 | <0.10 |  | <0.10 | <0.10 |  | 1.73 | 0.596 |  |
| #8, pH 8.0 |  | 9.59 |  | 0.0081 | <0.10 |  | <0.10 | <0.10 |  | 1.76 | 0.621 |  |
| #8, pH 9.0 |  | 9.50 |  | 0.0090 | <0.10 |  | <0.10 | <0.10 |  | 3.25 | 1.13 |  |
| #8, pH 10.0 |  | 10.0 |  | 0.0086 | <0.10 |  | <0.10 | <0.10 |  | 2.18 | 0.727 |  |
| #14, pH 2.0 |  | 2.01 |  | 0.0055 | 6.66 |  | 43.4 | 0.699 |  | 20.9 | 8.48 |  |
| #14, pH 3.0 |  | 3.74 |  | 0.0042 | 0.320 |  | 10.2 | 0.123 |  | 14.2 | 5.57 |  |
| #14, pH 4.0 |  | 7.30 |  | 0.0059 | <0.10 |  | <0.10 | <0.10 |  | 0.990 | 0.459 |  |
| #14, pH 5.0 |  | 8.37 |  | 0.0063 | <0.10 |  | <0.10 | <0.10 |  | 0.655 | 0.306 |  |
| #14, pH 6.0 |  | 8.48 |  | 0.0066 | <0.10 |  | <0.10 | <0.10 |  | 1.04 | 0.46 |  |
| #14, pH 7.0 |  | 8.45 |  | 0.0068 | <0.10 |  | <0.10 | <0.10 |  | 0.707 | 0.331 |  |
| #14, pH 8.0 |  | 8.45 |  | 0.0071 | <0.10 |  | <0.10 | <0.10 |  | 0.789 | 0.337 |  |
| #14, pH 9.0 |  | 8.71 |  | 0.0072 | <0.10 |  | <0.10 | <0.10 |  | 1.14 | 0.482 |  |
| #14, pH 10.0 |  | 9.34 |  | 0.0070 | <0.10 |  | <0.10 | <0.10 |  | 1.21 | 0.490 |  |
| #12C, pH 2.0 |  | 2.01 |  | 0.0241 | 0.346 |  | 3.26 | <0.10 |  | 3.85 | 1.08 |  |
| #12C, pH 3.0 |  | 3.04 |  | 0.0189 | <0.10 |  | 1.62 | <0.10 |  | 3.13 | 0.889 |  |
| #12C, pH 4.0 |  | 4.60 |  | 0.0136 | <0.10 |  | 0.285 | <0.10 |  | 1.69 | 0.553 |  |
| #12C, pH 5.0 |  | 5.03 |  | 0.0136 | <0.10 |  | <0.10 | <0.10 |  | 1.34 | 0.440 |  |
| #12C, pH 6.0 |  | 5.24 |  | 0.0136 | <0.10 |  | <0.10 | <0.10 |  | 1.23 | 0.405 |  |
| #12C, pH 7.0 |  | 5.04 |  | 0.0141 | <0.10 |  | <0.10 | <0.10 |  | 1.62 | 0.509 |  |
| #12C, pH 8.0 |  | 5.23 |  | 0.0136 | <0.10 |  | <0.10 | <0.10 |  | 1.57 | 0.416 |  |
| #12C, pH 9.0 |  | 5.91 |  | 0.0155 | <0.10 |  | <0.10 | <0.10 |  | 1.68 | 0.436 |  |
| #12C, pH 10.0 |  | 6.54 |  | 0.0140 | <0.10 |  | <0.10 | <0.10 |  | 2.63 | 0.547 |  |
| #16C, pH 2.0 |  | 1.99 |  | 0.0818 | 2.65 |  | 95.7 | <0.10 |  | 2.32 | 0.691 |  |
| #16C, pH 3.0 |  | 2.93 |  | 0.0390 | 2.27 |  | 85.7 | <0.10 |  | 2.20 | 0.641 |  |
| #16C, pH 4.0 |  | 3.35 |  | 0.0262 | 2.31 |  | 85.8 | <0.10 |  | 2.27 | 0.672 |  |
| #16C, pH 5.0 |  | 3.38 |  | 0.0270 | 2.27 |  | 83.9 | <0.10 |  | 2.23 | 0.659 |  |
| #16C, pH 6.0 |  | 3.32 |  | 0.0267 | 2.24 |  | 82.0 | <0.10 |  | 2.30 | 0.653 |  |
| #16C, pH 7.0 |  | 3.37 |  | 0.0274 | 2.25 |  | 81.9 | <0.10 |  | 2.42 | 0.651 |  |
| #16C, pH 8.0 |  | 3.38 |  | 0.0263 | 2.27 |  | 82.8 | <0.10 |  | 2.61 | 0.669 |  |
| #16C, pH 9.0 |  | 3.40 |  | 0.0129 | 2.17 |  | 78.5 | <0.10 |  | 3.19 | 0.646 |  |
| #16C, pH 10.0 |  | 3.41 |  | 0.0251 | 2.26 |  | 82.5 | <0.10 |  | 4.46 | 0.705 |  |
| Blank, pH 2.0 |  | - |  | <0.0002 | <0.10 |  | <0.10 | <0.10 |  | <0.10 | <0.10 |  |
| Blank, pH 3.0 |  | - |  | <0.0002 | <0.10 |  | <0.10 | <0.10 |  | <0.10 | <0.10 |  |
| Blank, pH 4.0 |  | - |  | <0.0002 | <0.10 |  | <0.10 | <0.10 |  | <0.10 | <0.10 |  |
| Blank, pH 5.0 |  | - |  | <0.0002 | <0.10 |  | <0.10 | <0.10 |  | <0.10 | <0.10 |  |
| Blank, pH 6.0 |  | - |  | <0.0002 | <0.10 |  | <0.10 | <0.10 |  | <0.10 | <0.10 |  |
| Blank, pH 7.0 |  | - |  | <0.0002 | <0.10 |  | <0.10 | <0.10 |  | 0.202 | <0.10 |  |
| Blank, pH 8.0 |  | - |  | <0.0002 | <0.10 |  | <0.10 | <0.10 |  | 0.363 | <0.10 |  |
| Blank, pH 9.0 |  | - |  | <0.0002 | <0.10 |  | 0.123 | <0.10 |  | 1.09 | <0.10 |  |
| Blank, pH 10.0 |  | - |  | <0.0002 | <0.10 |  | <0.10 | <0.10 |  | 2.29 | <0.10 |  |
| Se analyzed on 11-11-08 by method SW7742 |  |  |  |  |  |  |  |  |  |  |  |  |
| Other metals analyzed 11-7-08 by method SW6010B, |  |  |  |  |  |  |  |  |  |  |  |  |
| Extraction solutions prepared using H2SO4 and hydrated lime. |  |  |  |  |  |  |  |  |  |  |  |  |
| Samples extracted for 1 hour and then filtered through 0.45 um filter. |  |  |  |  |  |  |  |  |  |  |  |  |
| Extraction ratio: 2 g sample / 50 mL extractant |  |  |  |  |  |  |  |  |  |  |  |  |
| Table 2. Extractable Selenium Study |  |  |  |  |  |  |  |  |  |  |  |  |
| Sample ID | Extractant |  | Sample to Extractant |  |  | Filter Size |  |  | Selenium Concentration |  |  |  |
|  | pH |  | Ratio |  |  | (um) |  |  | mg/L |  |  |  |
| Blank | 9 |  | NA |  |  | 0.45 |  |  | 0.0002 |  |  |  |
| Blank | 9 |  | NA |  |  | 0.20 |  |  | <0.0002 |  |  |  |
| 14 | 9 |  | 0.5 g to 50 mL |  |  | 0.45 |  |  | 0.0024 |  |  |  |
| 14 | 9 |  | 0.5 g to 50 mL |  |  | 0.20 |  |  | 0.0023 |  |  |  |
| 14 | 9 |  | 1.0 g to 50 mL |  |  | 0.45 |  |  | 0.0044 |  |  |  |
| 14 | 9 |  | 1.0 g to 50 mL |  |  | 0.20 |  |  | 0.0044 |  |  |  |
| 14 | 9 |  | 2.0 g to 50 mL |  |  | 0.45 |  |  | 0.0083 |  |  |  |
| 14 | 9 |  | 2.0 g to 50 mL |  |  | 0.20 |  |  | 0.0079 |  |  |  |
| Se analyzed on 12-16-08 by method SW7742 |  |  |  |  |  |  |  |  |  |  |  |  |
| Extractant solution prepared using hydrated lime. |  |  |  |  |  |  |  |  |  |  |  |  |
| Samples extracted by tumbling for 1 hour. |  |  |  |  |  |  |  |  |  |  |  |  |

Figure 1,

Figure 2

Appendix

GFAA vs Hydride AF

GFAA (Graphite Furnace Atomic Absorption spectroscopy) is one of a few analytical techniques that is utilized to analyze for metals, such as selenium, in a variety of sample types.   This instrumentation for this method utilizes an electrically heated graphite tube furnace to provide the atomization energy required for absorbance based measurements.  This technique generally provides relatively low reporting capability for a variety of sample types.   Analytical bias, both positive and negative, can be an issue, particularly for complex matrices.   Prior to analysis, samples must be subjected to an appropriate digestion, typically involving the use of nitric acid and, for some samples, hydrogen peroxide.

Another technique for measuring selenium in a variety of sample types is hydride generation atomic fluorescence (HGAF).  This technique is very similar to method SW7742 (hydride generation atomic absorption) with the minor exception that a fluorescence detector is used in place of an absorbance based detector.   Just as with the GFAA technique, samples must first be digested before the instrumental based quantifying analysis can take place.   This digestion usually takes place in two steps; the first step involves a typical nitric acid digestion designed to solubilize selenium.  The second step requires heat and high concentrations of hydrochloric acid in order to convert (reduce) all selenium to the Se+4 oxidation state.  Selenium in this state is then measured and quantified by the HGAF technique.  This method provides very low reporting capability for selenium and is relatively robust in handling and overcoming matrix interferences which can cause analytical bias in many types of environmental samples.

It has been REIC’s experience that the HGAF technique provides superior low level reporting capability for selenium and is generally more robust at handling the complex matrices encountered in mining related samples.